## Slide 1: Fabrication of bilayered electrolyte Er0.5Bi1.5O3/Gd0.1Ce0.9O1.95 for low temperatures solid oxide fuel cells
Soukaina Mountadir, Victor Duffort, Rose-Noëlle Vannier
UCCS Laboratory – Team: MISSP
University of Lille – Villeneuve-d’Ascq
JNOEJC 2021 – 10th of June

## Slide 2: Operating principle of an SOFC
Converts the chemical energy
into electrical energy
∆Etheoretical
∆Eexperimental = ∆Etheoretical− RI−|ηanode| − |ηcathode|
Overall reaction :
2H2(g) +O2(g) 2H2O + heat + electricity
∆Etheoretical
2H2 (g) + 2O2- 2H2O(g)
Oxydation
O2 (g) + 4e- 2O2-
Reduction
Istomin et al. Russian Chemical Reviews 82(7) (2013) 686

## Slide 3
Good mechanical et chemical stability
Mediocre conductivity under 700°C
Mechanical instability, chemical reactivity, electrode microstructure
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
YSZ
A
4e-
Decreasing the operating temperature

## Slide 4
In order to decrease the operating temperature, two approaches are possible :
Decreasing the operating temperature
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
YSZ
A
4e-

## Slide 5
In order to decrease the operating temperature, two approaches are possible :
Decrease the electrolyte thickness
Limited
Decreasing the operating temperature
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
YSZ
A
4e-

## Slide 6
In order to decrease the operating temperature, two approaches are possible :
Decrease the electrolyte thickness
Limited
Electrolyte with a better ionic conductivity
Decreasing the operating temperature
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
YSZ
A
4e-

## Slide 7: Electrolytes for Low Temperature SOFC (LT-SOFC)
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
GDC
Cho et al., Electrochim. Acta, 56 (2011) 5472
A
4e-

## Slide 8: Electrolytes for Low Temperature SOFC (LT-SOFC)
Reduction Ce4+ Ce3+
Electronic contribution
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
GDC
e-
Cho et al., Electrochim. Acta, 56 (2011) 5472
A
4e-
Electrolyte | Thickness | Maximum power density mW.cm-2 at |  |  | OCV (V) 750°C
 |  | 650°C | 700°C | 750°C | 
GDC | 6 µm | 198 | 263 | 315 | 0,5

## Slide 9: Bilayered Electrolyte
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
GDC
YSZ
e-
Cho et al., Electrochim. Acta, 56 (2011) 5472
A
4e-
Electrolyte | Thickness | Maximum power density mW.cm-2 at |  |  | OCV (V) 750°C
 |  | 650°C | 700°C | 750°C | 
GDC | 6 µm | 198 | 263 | 315 | 0,5
YSZ/GDC | 330 nm / 6 µm | 188 | 430 | 587 | 0,67
YSZ/GDC | 1 µm / 6 µm | - | 301 | 438 | 1,05
YSZ blocks the
electronic contribution

## Slide 10
A
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
4e-
O2-
GDC
ESB
~ 5 µm
~ 10 µm
Ahn et al. Electrochem. Comm., 11 (2009) 1504
Wachsman, American Ceramic Society Bulletin, 39 (2014) 773
Maximum power density : 1.95 W.cm-2 at 650 °C with Bi2Ru2O7-ESB cathode
Operating temperature : 350°C with a Dy0,08W0,04Bi0,88O1,56 (DWSB) electrolyte
Bilayered Electrolyte

## Slide 11: OBJECTIVES
New cathode materials for low temperature SOFC
Cathode
Electrolyte
Anode
Air
Hydrogen
Water
O2-
GDC
ESB
ANR-BiBeLots
Densification of the ESB
Ni / GDC commercial half-cells with GDC
4e-

## Slide 12
1 µm
a)
b
c)
)
Synthesis – Erbium Stabilized Bismuth
SYNTHESIS : Bi1.5Er0.5O3 (ESB)
1 µm
1 µm
Coprecipitation
Citrate
10 µm
10 µm

## Slide 13
1 µm
a)
b
c)
)
Powder choice – Erbium Stabilized Bismuth
SYNTHESIS : Bi1.5Er0.5O3 (ESB)
1 µm
Citrate
10 µm
More reactive sintering
1 µm
Coprecipitation
10 µm
Grain expansion
Formation of grain boundaries
Elimination of porosity

## Slide 14
a)
b
c)
)
Powder choice – Erbium Stabilized Bismuth
SYNTHESIS : Bi1.5Er0.5O3 (ESB)
1 µm
Citrate
10 µm
ESB prepared with citrate method
Smaller grain size
Denser layer
Thinner layer
Grain expansion
Formation of grain boundaries
Elimination of porosity
More reactive sintering

## Slide 15
Ink preparation – Erbium Stabilized Bismuth
Binder
ESB (citrate) + dispersant + plasticizer
Powder choice
Low viscosity
Terpineol binder (EC3)
PolyVinyl Butyral binder (PVB)
280°C
450°C
High viscosity
Screen printing
Spin Coating

## Slide 16
Sintering – Erbium Stabilized Bismuth
Grain expansion
Formation of grain boundaries
Elimination of porosity

## Slide 17
Sintering – Erbium Stabilized Bismuth
20 µm
20 µm
800°C -3h
900°C -3h
GDC pellet with 2 layers of ESB deposited by screen printing and sintered at 800 °C
GDC pellet with 2 layers of ESB deposited by screen printing and sintered at 900 °C
Grain expansion
Formation of grain boundaries
Elimination of porosity

## Slide 18: Deposition methods – Erbium Stabilized Bismuth
GDC pellet with 2 layers of ESB sintered at 900 °C
20 µm
Screen Printer
Ink with Terpineol binder (EC3)
Shaban et al. J. Modern Trends in Phys. R., 14 (2014) 91

## Slide 19: Deposition methods – Erbium Stabilized Bismuth
GDC pellet with 2 layers of ESB sintered at 900 °C
GDC pellet with 2 layers of ESB sintered at 900 °C
20 µm
20 µm
Screen Printer
Spin Coater
Ink with Terpineol binder (EC3)
Shaban et al. J. Modern Trends in Phys. R., 14 (2014) 91

## Slide 20: Deposition methods – Erbium Stabilized Bismuth
GDC pellet with 2 layers of ESB sintered at 900 °C
GDC pellet with 2 layers of ESB sintered at 900 °C
20 µm
20 µm
Screen Printer
Spin Coater
Ink with Terpineol binder (EC3)
± 40 µm
± 20 µm
Interface problems
Good adhesion
Shaban et al. J. Modern Trends in Phys. R., 14 (2014) 91

## Slide 21: Deposition methods – Erbium Stabilized Bismuth
GDC pellet with 2 layers of ESB sintered at 900 °C
GDC pellet with 2 layers of ESB sintered at 900 °C
20 µm
20 µm
Screen Printer
Spin Coater
Ink with Terpineol binder (EC3)
Ink with PolyVinyl Butyl (PVB)
GDC pellet with 7 layers of ESB sintered at 900 °C
Interface problems
Good adhesion
20 µm
± 4 µm
Spin Coater
Shaban et al. J. Modern Trends in Phys. R., 14 (2014) 91
± 40 µm
± 20 µm

## Slide 22
Optimization of ESB deposition
?- 1h
900°C - 3h
? - 1h
280°C
450°C

## Slide 23
Optimization of ESB deposition
± 5 µm
450°C - 1h
900°C - 3h
280°C - 1h
1 µm
± 5 µm
10 µm
280°C
450°C

## Slide 24: CONCLUSION
Air
Hydrogen
Water
~ 5 µm
ESB
Densification of the ESB
GDC
~ 10 µm
A
4e-
ANR-BiBeLots

## Slide 25: CONCLUSION
Air
Hydrogen
Water
~ 5 µm
ESB
Densification of the ESB
GDC
~ 10 µm
A
4e-
ANR-BiBeLots
1 µm
Coprecipitation
Citrate
1 µm

## Slide 26: CONCLUSION
Air
Hydrogen
Water
~ 5 µm
ESB
Densification of the ESB
GDC
~ 10 µm
A
4e-
ANR-BiBeLots
1 µm
Coprecipitation
Citrate
1 µm
Deposition method: Spin Coating

## Slide 27: CONCLUSION
Air
Hydrogen
Water
~ 5 µm
ESB
Densification of the ESB
GDC
~ 10 µm
A
4e-
ANR-BiBeLots
1 µm
Coprecipitation
Citrate
1 µm
Two annealing steps at 280°C and 450°C
1 µm
± 5 µm
Deposition method: Spin Coating

## Slide 28: CONCLUSION
Air
Hydrogen
Water
~ 5 µm
ESB
Densification of the ESB
GDC
~ 10 µm
A
4e-
ANR-BiBeLots
1 µm
Coprecipitation
Citrate
1 µm
Two annealing steps at 280°C and 450°C
1 µm
± 5 µm
Deposition method: Spin Coating
ESB dense layer Cathode materials Complete cell

## Slide 29: THANK YOU FOR YOUR ATTENTION